***Sub Engineer***

1. For quality control of Portland cement, the test essentially done is

a. soundness

b. tensile strength

c. consistency

d. all the above.

Explanation: Option D is correct.

All the above test should be done for quality control. Because the setting time, soundness is very important.

2. If 1500 g of water is required to have a cement paste 1875 g of normal consistency, the percentage of water is,

a. 25%

b. 30%

c. 35%

d. 40%

Explanation: Option A is correct.

It's approximately 40%.
if we take 1500g water and 1875g cement then it will be 3375g cement paste so in this water/cement ratio will also be 0.44 and percentage of water is also 44%.
So, here option D is correct.

3. Under normal conditions using an ordinary cement, the period of removal of the form work, is :

a. 14 days for bottom slabs of spans 4.6 m and more

b. 21 days for bottom beams over 6 m spans

c. 2 days for vertical sides of columns

d. all the above.

Explanation: Option D is correct.

Option D wasn't correct because all vertical form work of column, wall and beams should be removed within 16-24 hours.

4. Wp and Wf are the weights of a cylinder containing partially compacted and fully compacted concrete. If the compaction factor  is 0.95, the workability of concrete is

a. very low

b. low

c. high

d. none of these.

Explanation: Option C is correct.

Extremely low - 0.65 to 0.68.
Very low - 0.75.
Low - 0.83 to 0.85.
Medium - 0.90 to 0.92.
High - 0.95.

5. For given water content, workability decreases if the concrete aggregates contain an excess of

a. flat particles

b. elongated particles

c. flaky paticles

d. all the above.

Explanation: Option D is correct.

Rounded shape particles are the most suitable for the high work-ability, but angular shape of aggregate is best for high strength b/c of good bonding between cement paste and aggregates.

6. M10 grade of concrete approximates

a. 1 : 3 : 6 mix

b. 1 : 1 : 2 mix

c. 1 : 2 : 4 mix

d. 1 : 1.5 : 3 mix

Explanation: Option A is correct.

M5 - 1:5:10
M7.5 - 1:4:8
M10 - 1:3:6
M15 - 1:1.5:3
M20 - 1:2:4
M25 - 1:1:2
M30 - 1:1:3

7. For ensuring quality of concrete, use

a. single sized aggegates

b. two sized aggregate

c. graded aggregates

d. coarse aggregates.

Explanation: Option C is correct.

Graded means a dive analysis practical mostly rounded particles USD but some of the pours due to used differently grading.

8. According to I.S. : 456, the number of grades of concrete mixes, is

a. 4

b. 5

c. 6

d. 7

Explanation: Option D is correct.

Ordinary concrete - M10 to M20.
Standard Concrete - M25 to M55.
High strength concrete - M60 - M80.

9. The mixture of different ingredients of cement, is burnt at

a. 1200°C

b. 1400°C

c. 1600°C

d. 1800°C

Explanation: Option B is correct.

In dry process, a temperature is 1400 - 1500 * C.
In wet process, the temperature is 1500 - 1600* C.

10. The risk of segregation is more for

a. wetter mix

b. larger proportion of maximum size aggregate

c. coarser grading

d. all the above.

Explanation: Option D is correct.

The risk of segreation is more for both coarse grading &larger proportion of coarse aggregate. But which one is have more risk.

11. After casting, an ordinary cement concrete on drying

a. expands

b. mix

c. shrinks

d. none of these.

Explanation: Option C is correct.

Concrete shrinks after drying due to the voids are filled by air after drying. It is considerably filled by water. Water will evaporate from that place by drying. . Thus it shrinks.

12. Hydration of cement is due to chemical action of water with

a. Tricalcium silicate and dicalcium silicate

b. Dicalcium silicate and tricalcium aluminate

c. Tricalcium aluminate and tricalcium alumino ferrite

d. All the above.

Explanation: Option D is correct.

These four Bogues compound are formed during chemical reaction of cement with water. Even type of cement is also decided by varying the percentage of these four bogues compound.

13. To obtain cement dry powder, lime stones and shales or their slurry, is burnt in a rotary kiln at a temperature between

a. 1200° and 1300°C

b. 1300° and 1400°C

c. 1400° and 1500°C

d. 1500° and 1600°C

Explanation: Option C is correct.

1300° to 1500° for mixing of constitute,
Here bogues compound formed;
1500° to 1600°  To obtain a dry powder.

14. Permissible compressive strength of M 300 concrete grade is

a. 150 kg/cm2

b. 200 kg/cm2

c. 250 kg/cm2

d. 300 kg/cm2

Explanation: Option D is correct.

As per latest technology M200 and M400 grade of concrete is using in other country like Canada and New Zealand.

15. The standard sand now a days used in India, is obtained from

a. Jullundur (Punjab)

b. Hyderabad (Andhra Pradesh)

c. Ennore (Madras)

d. Cuttuck (Orissa).

Explanation: Option C is correct.

16. The maximum amount of dust which may be permitted in aggregates is

a. 5% of the total aggregates for low workability with a coarse grading

b. 10% of the total aggregates for low workability with a fine grading

c. 20% of the total aggregates for a mix having high workability with fine grading

d. all the above.

Explanation: Option D is correct.

By replacing sand with dust strength increases. We have performed this test in the lab. We replaced the sand with crusher dust and as we were increasing the percentage of dust the corresponding strength also increased.

17. Proper proportioning of concrete, ensures

a. desired durability

b. water tightness of the structure

c. resistance to water

d. all the above.

Explanation: Option D is correct.

18. The bulk density of aggregates does not depend upon :

a. specific gravity of aggregates

b. grading of aggregates

c. size and shape of the container

d. none of these.

Explanation: Option C is correct.

Bulk density is dependent upon the properties of the aggregates which are the size, shape, specific gravity of aggregates. It is independent of the container.

19. Curing

a. reduces the shrinkage of concrete

b. preserves the properties of concrete

c. prevents the loss of water by evaporation

d. all of the above.

Explanation: Option D is correct.

Actually, the crack is formed due to the heat of hydration in the structure (members) so this heat is reduced by curing.

20. While compacting the concrete by a mechanical vibrator, the slump should not exceed

a. 5.0 cm

b. 7.5 cm

c. 10 cm

d. 15 cm

Explanation: Option A is correct.

Low workability- (25mm-50mm) slump- light reinforcement requires mechanically operated vibrator.
Medium workability- (50mm-100mm) slump- standard reinforcement requires hand-operated vibrator.

21. Construction joints are provided

a. where the member is supported by other member

b. at 18 m apart in huge structures

c. in concrete wall at sill level of windows

d. all the above.

Explanation: Option D is correct.

Because the place where bm and shear force is minimum there will be less displacement to the structure which meets with the point that we can easily provide construction joint in that place.

22. An aggregate is said to be flaky if its least dimension is less than

a. 2/5th of mean dimension

b. 3/5th of mean dimension

c. 4/5th of mean dimension

d. none of these.

Explanation: Option B is correct.

In other words we can say that an aggregate is said to be flaky if its least dimension is less than 0.6 times of mean dimension.

23. The following proportion of the ingredients of concrete mix, is not in conformation to arbitrary method of proportioning

a. 1 : 2 : 4

b. 1 : 3 : 6

c. 1 : 2 : 8

d. 1 : 4 : 10

Explanation: Option D is correct.

Arbitrary Method of proportioning of concrete:.
The general expression for the proportions of cement, sand and coarse aggregate is 1 : n : 2n by volume. So, option C and D both are wrong.

24. The increased cohesiveness of concrete, makes it

a. less liable to segregation

b. more liable to segregation

c. more liable to bleeding

d. more liable for surface scaling in frosty weather

Explanation: Option A is correct.

Cohesion means molecular attraction between same type of material.
In different type of material molecular attraction is adhesion.

25. The ratio of the length to breadth of a wooden float, is

a. 5.5

b. 6.5

c. 7.5

d. 8.5

Explanation: Option C is correct.

Wooden float is also known as skimming float. It has a thickness of about 10-12 mm. It is used for the finishing coat of the plaster.

26. To ensure constant moisture content in aggregates

a. height of each aggregate pile should not exceed 1.50 m

b. aggregate pile should be left for 24 hours before aggregates are used

c. conical heaps of aggregates should be avoided to prevent moisture variation

d. all the above.

Explanation: Option D is correct.

AGGREGATE PILR: Dumping of AGGREGATE in a cone shape before it is used for roofing or any other works at the sites.

27. Workability improved by adding

a. foaming agent

b. oily-agent

c. aluminium compound

d. all the above.

Explanation: Option D is correct.

28. The commonly used material in the manufacture of cement is

a. sand stone

b. slate

c. lime stone

d. graphite.

Explanation: Option C is correct.

29. If 20 kg of coarse aggregate is sieved through 80 mm, 40 mm, 20 mm, 10 mm, 4.75 mm, 2.36 mm, 1.18 mm, 600 micron, 300 micron and 150 micron standard sieves and the weights retained are 0 kg, 2 kg, 8 kg, 6 kg, 4 kg respectively, the fineness modulus of the aggregate, is

a. 7.35

b. 7.40

c. 7.45

d. none of these.

Explanation: Option B is correct.

The fm of coarse aggregate is C+500/100.
The fm of fine aggregate is f/100.
So, what we try  on sieve 4.75 lower all are fine particles as per code.

30. Curing a concrete for long period ensures better

a. strength

b. water resistance

c. water tightness and durability

d. all the above.

Explanation: Option D is correct.

31. For the construction of cement concrete floor, the maximum permissible size of aggregate, is

a. 6 mm

b. 8 mm

c. 10 mm

d. 12 mm

Explanation: Option C is correct.

40 mm for massive works like dams, retaining walls, etc.
20 mm for Reinforced member.
10 mm for floor.

32. The process of proper and accurate measurement of concrete ingredients for uniformity of proportion, is known

a. curing

b. mixing

c. batching

d. none of these.

Explanation: Option C is correct.

33. Pick up the correct statement from the following:

a. Insufficient quantity of water makes the concrete unworkable

b. Excess quantity of water makes the concrete segregated

c. Excess quantity of water causes bleeding in concrete

d. All the above.

Explanation: Option D is correct.

Segregation means the Coarse aggregates settled down which is type 1 segregation.
Even bleeding is also a type of segregation which is type 3 segregation.
Type 2 will be escaping of grout while doing hand mixing.

34. The preliminary test is repeated if the difference of compressive strength of three test specimens, exceeds

a. 8 kg/cm2

b. 10 kg/cm2

c. 12 kg/cm2

d. 15 kg/cm2

Explanation: Option D is correct.

AS PER IS-456 "The test results of the sample shall be the average of the strength of three specimens".
The individual variation should not be more than +15 percent of the average. If more, the test results of the sample are invalid.

35. Pick up the correct proportions of chemical ingredients of cement

a. Lime : Silica : Alumina : Iron oxide : 63 : 22 : 6 : 3

b. Silica : Lime : Alumina : Iron oxide : 63 : 22 : 6 : 3

c. Alumina : Silica : Lime : Iron oxide : 63 : 22 : 6 : 3

d. Iron oxide : Alumina : Silica : Lime : 63 : 22 : 6 : 3

Explanation: Option A is correct.

Lime - 62%.
Silica - 22%.
Alumina - 5%.
Iron oxide - 4%.
Magnesium oxide - 3%.
Sulphur - 2%.
Alkalines - 1%.

36. Transport of concrete by pumps, is done for a distance of

a. 200 m

b. 300 m

c. 400 m

d. none of these.

Explanation: Option C is correct.

The effective pumping distance:
300-1000ft for horizontal.
100-300ft for vertically.
So 400m is right option.
Refence book - Concrete Construction Engineering by Edward G. Nawy.

37. If X, Y and Z are the fineness modulli of coarse, fine and combined aggregates, the percentage (P) of fine aggregates to combined aggregates, is

a.

b.

c.

d.

Explanation: Option A is correct.

38. Slump test is done for

a. clay

b. sand

c. lime

d. concrete.

Explanation: Option D is correct.

39. The high strength of rapid hardening cement at early stage, is due to its

a. finer grinding

b. burning at high temperature

c. increased lime cement

d. higher content of tricalcium.

Explanation: Option C is correct.

Finer grinding and tricalcium aluminate C3A causes rapid hardening.
While early strength is given to the cement by tricalcium silicate C3S.

40. Pick up the correct statement from the following:

a. Water and aggregates are measured in litres

b. The finished concrete is measured in cubic metres

c. 20 bags of cement make one tonne

d. All the above.

Explanation: Option D is correct.

Option b is also correct.
As 1529.20 kg  = 1 m3.
So, we can convert kg into m3 and then we easily convert m3 into litres.

41. Concrete mainly consists of

a. aggregates

b. admixture

c. water

d. all the above.

Explanation: Option D is correct.

Admixture is not a mandatory component of concrete.
But, now a days, it is broadly used in concrete to meet specific purposes.

42. Vicat's apparatus is used for

a. consistency test

b. setting time test

c. soundness test

d. compressive strength test.

Explanation: Option A is correct.

Vicat apparatus is used for initial, final setting time and std consistency test so option B & C is correct.

43. M 150 grade of concrete approximates

a. 1 : 1 :2 mix

b. 1 : 2 : 4 mix

c. 1 : 1.5 : 3 mix

d. none of these.

Explanation: Option B is correct.

M10 - 1:3:6.
M15 - 1:2:4.
M20 - 1:1.5:3.
M25 - 1:1:2.
          1:4:8
M30 - 1:5:10
           1:6:12.
M35 - post-tensioned prestressed concrete.
M40 - pre-tensioned prestressed concrete.

44. Workability of concrete is measured by

a. Vicat apparatus test

b. Slump test

c. Minimum void method

d. Talbot Richard test.

Explanation: Option B is correct.

Work ability of concrete is measured by slump cone test, compaction factor test.
Slump cone is used for medium work ability. For high work abilities it is not accurate.
Slump values vary from 0 mm to 300 mm.

45. The rock which is not calcareous, is :

a. macl

b. chalk

c. laterite

d. none of these.

Explanation: Option C is correct.

46. Internal friction between the ingredients of concrete, is decreased by using

a. fine aggregates

b. rich mix

c. more water and coarse aggregates

d. none of these.

Explanation: Option C is correct.

How, if we increase water so there will be less work ability and slump value. This is not a way to reduce internal friction we must use some special ingredients.

47. For road pavements, the cement generally used, is

a. rapid hardening cement

b. low heat cement

c. blast furnace slag cement

d. none of these.

Explanation: Option A is correct.

Rapid hardening is correct because the road is open to traffic in minimum days and it also have one day strength equal to 3 day strength of opc.

48. Construction joints are generally provided in concrete

a. retaining walls

b. lining of canals

c. lining of tunnels

d. all the above.

Explanation: Option D is correct.

49. Separation of coarse aggregates from mortar during transportation, is known

a. creeping

b. segregation

c. shrinkage

d. none of these.

Explanation: Option B is correct.

Labour is placed to the concrete in slab some force to be thrown away particles will be separated is called segregation.

50. According to the recommendations of IS : 456-1978, the expansion joints

a. are provided to ensure minimum resistance

b. are supported on separate columns

c. do not carry reinforcement across them

d. all the above.

Explanation: Option D is correct.

Option D is not correct because the dowel bar is provided in the expansion joint. Only in contraction joint, there is no reinforcement.

51. Grading of sand causes great variation in

a. strength of concrete

b. durability of concrete

c. handing and placing of concrete

d. all the above.

Explanation: Option D is correct.

52. Shrinkage in concrete can be reduced by using

a. less cement in the concrete

b. proper concrete mix

c. presaturated aggregates

d. all the above.

Explanation: Option D is correct.

Increase of the water content by one percent will approximately increase the drying shrinkage by three percent.

53. Ordinary concrete is not used for concrete grade

a. M 150

b. M 200

c. M 250

d. M 400

Explanation: Option D is correct.

M10 to  20 - Ordinary concrete mix.
M25 to M55 - Standard concrete mix.
M60 to M60 - high strength concrete mix.

54. 1.S. Sieve Nos. 10 mm and 4.75 mm are geneally used for grading of

a. fine aggregates

b. neither (a) nor (b)

c. both (a) and (b)

d. none of these.

Explanation: Option C is correct.

The aggregate of size more than 75 mm are called Cyclopean aggregate. Since the Max size of coarse aggregate is 75 mm.

55. Pick up the correct statement from the following:

a. The free water is the amount of water added while mixing and the amount of water held on the surface of the aggregates prior to mixing

b. The total water is the free water and the amount actually absorbed by the aggregates

c. Neither (a) nor (b)

d. Both (a) and (b).

Explanation: Option D is correct.

Free water is the amount of water that is susceptible to the gravitational force. In other words, the water that is unaffected by the surface force.

56. Addition of pozzolana to ordinary port land cement, causes

a. reduction in chemical action with sulphates

b. increase in shrinkage

c. reduction bleeding

d. all the above.

Explanation: Option D is correct.

The addition of pozzolana to ordinary Portland cement increases shrinkage but reduces the permeability of the concrete. It increases the elastic modulus of concrete. Less heat of hydration. Offers greater resistance to aggressive weather.

57. Too wet concrete may cause

a. excessive laitance

b. segregation

c. lower density

d. all the above.

Explanation: Option D is correct.

Laitance is a weak, easily-crumbled layer on the surface of concrete, consisting of cement and fine aggregates that rise to the surface when too much water is added. Laitance may also be caused by over-trowelling, rain damage, or poor curing.

58. Addition of pozzolana to cement causes

a. loss of heat of hydration

b. reduction in bleeding

c. increase in curing time

d. all the above.

Explanation: Option D is correct.

59. Hardening of cement occurs at

a. rapid rate during the first few days and afterwards it continues to increase at a decreased rate

b. slow rate during the first few days and afterwards it continues to increase at a rapid rate

c. uniform rate throughout its age

d. none of these.

Explanation: Option D is correct.

Hardness of cement occurs with in 30 minutes to 600 minutes (10 hours).
As Hardness of Cement or Concrete is due to from their Initial and final setting times.

60. Pick up the correct statement from the following:

a. Silica in excess, causes the cement to set slowly

b. Alumina in excess, reduces the strength of the cement

c. Magnesium oxide in excess, remains in free state and makes the cement unsound

d. All the above.

Explanation: Option D is correct.

61. Batching error means inaccuracy in the quantity of

a. aggregates

b. cement

c. water

d. all the above.

Explanation: Option D is correct.

62. Pick up the correct statement from the following i.

a. Higher workability indicates deficiency of sand

b. If the concrete mix is dry, the slump is zero

c. Concrete mix having zero slump, is unsuitable for high strength.

d. All the above.

Explanation: Option D is correct.

No, Option C may be wrong.
In My point of view, if the concrete is dry (i.e., low), the slump value ranges from 25 to 75. It may not be necessarily zero.

63. You are asked to construct a massive dam, the type of cement you will use, is

a. rapid hardening cement

b. low heat cement

c. blast furnace slag cement

d. white cement.

Explanation: Option B is correct.

The quick setting is cement generally used in under running water and for construction of massive dams, we will use generally low heat Portland cement.

64. The produce impermeable concrete

a. proper compaction of concrete is required

b. proper curing of concrete is required

c. properly graded and non-porous aggregates are requied

d. all the above.

Explanation: Option D is correct.

65. Water required per bag of cement, is

a. 14 kg

b. 21 kg

c. 28 kg

d. 35 kg

Explanation: Option D is correct.

Simple,
Vol of cement bag of 50 Kg = 0.035 m3.
And, per 1 m3 we need 1000Kg of water.
So, Water required = 1000*0.035 = 35 Kg.
Since there is no mention about w/c ratio.

66. Pick up the incorrect statement from the following:

a. The axis of the mould is perpendicular to the end faces

b. The internal surface of the mould is kept clean and free from set cement

c. The mould is in the form of a frustum of hexagonal pyramid

d. None of these.

Explanation: Option C is correct.

67. ISI has specified full strength of concrete after

a. 14 days

b. 21 days

c. 28 days

d. none of these.

Explanation: Option D is correct.

Days -- Concrete Percentage.
1  -- 16%.
3  -- 45%.
7  --  65%.
14  --  90%.
28 --  99%.

68. For construction of structures in sea water, the cement generally preferred to, is

a. Portland-pozzolana cement

b. quick setting cement

c. low heat Portland cement

d. rapid hardening cement

Explanation: Option A is correct.

Portland pozzolana cement is used under water constructions.
1) Pozzolana causes impermeability.
2) pozzolana resist chemical and sulphide attack.

69. Percentage of pozzolanic material containing clay upto 80% used for the manufacture of pozzolana cement, is

a. 30%

b. 40%

c. 50%

d. 60%

Explanation: Option A is correct.

70. For batching 1:3:6 concrete mix by volume, the ingredients required per bag of 50 kg cement, are:

a. 70 kg of sand and 140 litres of aggregates

b. 105 litres of sand and 140 litres of aggregates

c. 105 litres of sand and 210 litres of aggregates

d. none of these.

Explanation: Option C is correct.

1kg = 0.7 liters.
50kg cement - 35liters.
3*50kgsand-150 * .7 = 105liter.
300kg aggregate-300*.7 = 210 liters.

71. The process of hardening the concrete by keeping its surface moist is known

a. wetting

b. curing

c. compacting

d. none of these.

Explanation: Option B is correct.

72. The grade of concrete not recommended by I.S. : 456, is

a. M 200

b. M 300

c. M 400

d. M 500

Explanation: Option D is correct.

According to IS 456:2000.
The concrete mixes are designated into 7 grade:
M10,
M15,
M20,
M25,
M30,
M35,
and M40.

73. C.R.R.I. charts are used to obtain a relatioship between strength of concrete and

a. water cement ratio

b. workability

c. grading of aggregate

d. fineness modulus

Explanation: Option A is correct.

1) The span to depth ratio for a cantilever of the beam should not exceed 7.
2) Also, the maximum size of cantilever provided should be 10m.
3) i.e length of the cantilever should not be more than 10 meters.

74. Proper batching ensures

a. durability

b. workability

c. strength

d. all the above.

Explanation: Option D is correct.

75. Workability of concrete for a given water content is good if the aggregates, are

a. rounded aggregate

b. irregular aggregate

c. angular aggregate

d. flaky aggregates.

Explanation: Option A is correct.

Angular aggregate is best option than rounded aggregate. But the rounded aggregate is also used so, I agree.

76. Pick up the correct statement from the following:

a. Fine sand bulks more than coarse sand

b. With 10% moisture content by weight, the bulking of sand is increased by 50%.

c. The volume of fully saturated sand, is equal to the volume of dry and loose sand

d. All the above.

Explanation: Option D is correct.

77. For compacting plain concrete road surface of thickness less than 20 cm, we use

a. internal vibrator

b. screed vibrator

c. form vibrator

d. none of these.

Explanation: Option B is correct.

<20 cm then use screed vibrator.
>60 cm then use needle vibrator.
These are for road surface only.

78. Pick up the correct statement from the following:

a. Expansion joints are provided to accommodate thermal expansion

b. Construction joints are provided to control shrinkage cracks

c. Expansion joints need not be provided in foundation concrete

d. All the above.

Explanation: Option D is correct.

79. Pick up the correct statement from the following:

a. Consistency does not affect the workability of concrete

b. If the slump increases, workability decreases

c. If the concrete mix is dry, the slump is maximum

d. None of these.

Explanation: Option D is correct.

The Segregation decreases the with workability.
Workability is affected by consistency.
If the concrete mix is dry, the slump will be minimum.

80. Specified compressive strengh of concrete is obtained from cube tests at the end of

a. 7 days

b. 14 days

c. 21 days

d. 28 days.

Explanation: Option D is correct.

81. An aggregate is said to be flaky, if its least dimension is less than

a. 3/4 mean dimension

b. 3/5 mean dimension

c. 5/8 mean dimension

d. none of these.

Explanation: Option B is correct.

82. Pick up the incorrect statement from the following:

a. A rich mix of concrete possesses higher strength than that a lean mix of desired workability with excessive equantity of water

b. The strength of concrete decreases as the water cement ratio increases

c. If the water cement ratio is less than 0.45, the concrete is not workable and causes honey-combed structure

d. Good compaction by mechanical vibrtions, increases the strength of concrete

Explanation: Option A is correct.

For the same strength, the water content and cement will be less in rich mixes so chances of excessive water are more in lean concrete. Hence A is incorrect.

83. The percentage of the aggregate of F.M. 2.6 to be combined with coarse aggregate of F.M. 6.8 for obtaining the aggregates of F.M. 5.4, is

a. 30%

b. 40%

c. 50%

d. 60%.

Explanation: Option C is correct.

Here, The percentage of the aggregate of F.M. 2.6 to be combined.
i.e  If the total amount of F.M 2.6 is 100% now then how much % of Aggregate will be required to obtain an F.M 5.4 with 100% amount of F. M. 6.8 aggregates.

84. The final operation of finishing floors, is known as

a. floating

b. trowelling

c. finishing

d. all the above.

Explanation: Option B is correct.

Floating: It is the process of removing the irregularities from the surface of concrete left after screeding.

85. The internal dimensions of a ware house are 15 m x 5.6 m, and the maximum height of piles is 2.70 m, the maximum number of bags to be stored in two piles, are

a. 2000 bags

b. 2500 bags

c. 3000 bags

d. 4000 bags

Explanation: Option C is correct.

Width of gallery = .6m,
So, width of warehouse = 5.6 - .6 = 5.
Now volume=15 * 5 * 2.7 = 202.5.
Now, the volume of one bag=.054.
So, 202.5/.054 = 3750 bags.

86. For an ordinary Portland cement

a. soundness varies from 5 to 10 mm

b. initial setting time is not less than 30 minutes

c. compressive stress after 7 days, is not less than 175 kg/cm2

d. all the above.

Explanation: Option B is correct.

Those who agree with option E, they also agree that option C is correct for OPC, but those who are saying option C is correct they are not defining why option E is incorrect. As A, B, C, D all are the necessary criteria for OPC.

87. The maximum thickness of concrete floor of a cement warehouse, is

a. 15 cm

b. 20 cm

c. 25 cm

d. 30 cm

Explanation: Option C is correct.

88. A construction joint is provided where

a. bending moment is small

b. shear force is small

c. the member is supported by other member

d. all the above.

Explanation: Option D is correct.

How it could, as sf is smaller or zero bm on the other hand is greater and max at zero sf. So we can't choose them at z same time.

89. The compaction of concrete, improves

a. density

b. strength

c. durability

d. all the above.

Explanation: Option D is correct.

90. Pick up the correct statement from the following:

a. Water cement paste hardens due to hydration

b. During hardening cement binds the aggregates together

c. Cement provides strength, durability and water tightness to the concrete

d. All the above.

Explanation: Option D is correct.

91. The light weight aggregates are obtained from

a. sedimentary rocks

b. metamorphic rocks

c. igneous rocks

d. volcanic source.

Explanation: Option D is correct.

Volcanic rock manufactured when melting magma comes on the top. The surface of the earth and deposited. Example basalt and trap.
And it is light in weight.

92. If the depth of moist sand in a cylinder is 15 cm and the depth of the sand when fully inundated with water is 12 cm, the bulking of the moist sand, is

a. 12%

b. 15%

c. 20%

d. 25%.

Explanation: Option D is correct.

Formula isn't required.
It's % bulking of sand = what percentage of inundated sand, the bulking happened.
Therefore, = (bulked mass / inundated mass)*100.
= (15-12)*100/12.
= 25%.

93. Pick up the correct statement from the following:

a. According to the petrological characteristics, concrete aggregates are classified as heavy weight, normal weight and light weight

b. According to the shape of the particles, concrete aggregates are classified as rounded irregular, angular and flaky

c. According to the surface texture of the particles, the concrete aggregates are classified as glassy, smooth, granular, rough, crystalline, honey combed and porous

d. All the above.

Explanation: Option D is correct.

94. Segregation is responsible for

a. porous layers in concrete

b. surface scaling in concrete

c. sand streaks in concrete

d. all the above.

Explanation: Option D is correct.

95. Addition of pozzolana to cement

a. increases strength

b. increases heat of hydration

c. decreases curing time

d. none of these.

Explanation: Option D is correct.

It increase the long term strength due to forming CSH which is stronger, and through better backing of concrete.

96. The datum temperature for maturity by Plowman, is

a. 23°C

b. 0°

c. - 5.6°C

d. - 11.7°C

Explanation: Option D is correct.

97. Pick up the incorrect statement from the following:

a. The process of changing cement paste into hard mass, is known as setting of cement

b. The phenomenon by virtue of which cement does not allow transmission of sound, is known as soundness of cement

c. The heat generated during chemical reaction of cement with water, is known as heat of hydration

d. None of these.

Explanation: Option B is correct.

Option C is correct.
As by conducting sounds test (Le-chatleirs apparatus) we can find the changes in volume.

98. Permissible compressive strength of M 150 concrete grade is

a. 150 kg/cm2

b. 200 kg/cm2

c. 250 kg/cm2

d. 300 kg/cm2

Explanation: Option A is correct.

Here, permissible strength is required to be determine fck 150 is already given. So, permissible strength= fck/partial safety factor.
150/1.5 = 100 kg/sq.cm.
fck = characteristic compressive strength of concrete at 28 days after curing.

99. Slump test of concrete is a measure ofits

a. consistency

b. compressive strength

c. tensile strength

d. impact value.

Explanation: Option A is correct.

The concrete slump test measures the consistency of fresh concrete before it sets. It is performed to check the workability of freshly made concrete.

100. Pozzolana cement is used with confidence for construction of

a. massive foundations

b. abutments

c. R.C.C. structures

d. all the above.

Explanation: Option D is correct.

Pozzolana cement is a low heat cement It's hardening properties are slow in 28 days but after this it can gain streangth like normal ppc so it can use in massive structures as dams, abutment, Massive foundation etc.

101. Water cement ratio is

a. weight of water to that of cement

b. weight of concrete to that of water

c. volume of concrete to that of water

d. both (a) and (b) of the above.

Explanation: Option D is correct.

Actually 1m3 of the volume contain 1000 kg of water or 1000 liters of water. So both weight and volume will be correct.

102. Efflorescence in cement is caused due to an excess of

a. iron oxide

b. silica

c. alkalis

d. magnesium oxide.

Explanation: Option C is correct.

Due to the presence of N2O and K3O which is soda and potash emerge on the surface as the moisture vaporized.

103. If the engineer-in-charge approves, the 10 cm cubes may be used for the work test of concrete provided maximum nominal size of aggregate, does not exceed

a. 15 cm

b. 20 cm

c. 25 cm

d. 30 cm

Explanation: Option B is correct.

For 10 cm cube size of aggregate 20mm or less and for 15 cm cube size of aggregate more than 20mm is used.

104. The diameter of the Vicat plunger is 10 mm and its length varies from

a. 30 mm to 40 mm

b. 40 mm to 50 mm

c. 50 mm to 60 mm

d. none of these.

Explanation: Option B is correct.

5mm diameter plunger is not used in Vicat plunger.
10 mm diameter plunger- for consistency.
1 mm sq c/s - for initial setting time and 1 mm c/s with 5mm annular collar- for the final setting time.

105. The shrinkage of concrete

a. is proportional to water content is the mix

b. is proportional to cement concrete

c. increases with age of concrete

d. all the above.

Explanation: Option D is correct.

106. The ratio of various ingredients (cement, sand, aggregates) in concrete of grade M 200, is

a. 1 : 3 : 6

b. 1 :   : 3

c. 1 : 1 : 2

d. 4 : 2 : 1

Explanation: Option B is correct.

M20 is 20 N/mm2 and M200 is 200 kg/cm2.
For M20 or M200 grade.
Cement : Sand : Aggregate == 1:1.5:3.

107. Separation of water or water sand cement from a freshly concrete, is known

a. bleeding

b. creeping

c. segregation

d. flooding

Explanation: Option A is correct.

Bleeding is a form of segregation in which water present in the concrete mix is pushed upwards due to the settlement of cement and aggregate.

108. Slump test of concrete is a meausre ofits

a. consistency

b. compressive strength

c. tensile strength

d. impact value.

Explanation: Option A is correct.

109. According to Water-Cement Ratio Law, the strength of workable plastic concrete

a. depends upon the amount of water used in the mix

b. does not depend upon the quality of cement mixed with aggregates

c. does not depend upon the quanity of cement mixed with aggregates

d. all the above.

Explanation: Option D is correct.

Abram equation only gives the relation b/w strength and water required. It doesn't talk about quality.

110. Pick up the incorrect statement from the following:

a. In properly graded aggregates, bulk density is more

b. In single size aggregates, bulk density is least

c. In single size aggregates, bulk density is maximum

d. None of these.

Explanation: Option C is correct.

Properly Graded size aggregate would occurs maximum bulk density.
And also we use this for obtaining dense concrete.

111. Saw dust can be rendered chemically inert by boiling it in water containing

a. ferrous sulphate

b. potassium chloride

c. ammonia

d. nitric acid

Explanation: Option A is correct.

112. Pick up the correct statement from the following:

a. High percentage of C3S and low percentage of C2S make the cement less resistive to chemical attack

b. Low percentage of C3S and high percentage of C2S contribute to slow hardening

c. Low percentage of C3S and high percentage of C2S provide greater resistance to chemical attack

d. All the above.

Explanation: Option D is correct.

C3S = initial strength of concrete in 28 days.
C2S= final strength of concrete that is the ultimate strength.
C3A = initial setting time of concrete.
C4AF= a final setting time of concrete.

113. The factor which affects workability, is

a. shape and size of the aggregates

b. grading and surface textures of the aggregates

c. air entraining agents

d. all the above.

Explanation: Option D is correct.

114. The cement whose strength is a little lower than the ordinary cement during the first three months but attains afterwards the same strength, is known as

a. low-heat Portland cement

b. rapid hardening Portland cement

c. Portland blast slag cement

d. Portland pozzolana cement

Explanation: Option A is correct.

Disadvantages of Low Heat Cement:
Initial strength gained is lower than that of OPC concrete, but the final strength is the same as that of OPC.

115. Pick up the correct statement from the following:

a. Concrete using sand stones, cracks due to excessive shrinkage

b. Very hard and close grained crystallined lime stones are suitable aggregates but provide low strength

c. Broken bricks produce a concrete having good fire resisting qualities

d. All the above.

Explanation: Option D is correct.

116. Pick up the correct statement from the following:

a. Water lubricates the mixture of gravel, sand and cement

b. Only a small quantity of water is required for hydration of cement

c. Strength of concrete structure largely depends upon its workability

d. All the above.

Explanation: Option D is correct.

Yes, there is a small qty of water required for hydration i.e 0.23. and further workability is increased by PCE admixture if required.

117. Pick up the incorrect statement applicable to the field test of good cement.

a. The colour of the cement is bluish

b. A handful of cement thrown into a bucket of water should sink immediately

c. By rubbing cement in between fingers, one should feed rough

d. All the above.

Explanation: Option D is correct.

As cement's SP gravity is more than that of water hence it should sink in water when thrown into a bucket of water.

118. Pick up the correct statement from the following:

a. Gypsum (calcium sulphate) acts as an accelerator

b. Gypsum (calcium sulphate) acts as a retarder

c. Calcium chloride acts as an accelerator

d. Both (c) and (d).

Explanation: Option D is correct.

119. Joints in concrete structures, are provided

a. to reduce the tensile stresses likely to be developed due to evaporation of water

b. to minimise the change in the dimensions of the slab

c. to minimise the necessary cracking

d. all the above.

Explanation: Option D is correct.

120. If the effective working time is 7 hours and per batch time of concrete is 3 minutes, the output of a concrete mixer of 150 litre capacity, is

a. 15, 900 litres

b. 16, 900 litres

c. 17, 900 litres

d. 18, 900 litres

Explanation: Option D is correct.

Effective working time= 7 hours = 7*60 = 420 minute.
Per batch time = 3 minute.
Number of mixing batch = 420/3 = 140.
Output concrete of per batch = 150 litre.
Output concrete 140 batch = 140*150 = 21000 litre.

121. The condition not applicable to water cement ratio law, is

a. concrete specimens may be tested at any temperature

b. concrete specimens need be of same age

c. concrete specimens need be of same size

d. none of these.

Explanation: Option A is correct.

122. High temperature

a. increases the strength of concrete

b. decreases the strength of concrete

c. has no effect on the strength of concrete

d. none of these.

Explanation: Option B is correct.

Is it mentioned here, that dehydration is occurring. And In labs, a high temperature of water increases strength.

123. The bulk density of aggregates, is generally expressed as

a. kg/cubic metre

b. kg/litre

c. g/cm3

d. none of these.

Explanation: Option B is correct.

Kg/m^3 is linear density or simply density. Bulk density is related to liquid density and is, therefore, kg/litre.

124. The grade of concrete M 150 means that compressive strength of a 15 cm cube after 28 days, is

a. 150 kg/cm2

b. 200 kg/cm2

c. 250 kg/cm2

d. 300 kg/cm2

Explanation: Option A is correct.

125. Allowable shear strength of concrete, depends upon

a. shear strength

b. tensile strength

c. compressive strength

d. none of these.

Explanation: Option A is correct.

126. The most useless aggregate is one whose surface texture is

a. smooth

b. granular

c. glassy

d. honey combed and porous.

Explanation: Option C is correct.

127. To obtain a very high strength concrete, use very fine grained

a. Granite

b. Magnetite

c. Barite

d. Volcanic scoria.

Explanation: Option A is correct.

Granite is the igneous rock which when graded produces high strength coarse aggregate so it may be A.

128. Concrete containing

a. silicious aggregates, has higher co-efficient of expansion

b. igneous aggregates, has intermediate coefficient of expansion

c. lime stones, has lowest co-efficient of expansion

d. All the above.

Explanation: Option D is correct.

129. An ordinary Portland cement when tested for its fineness, should not leave any residue on I.S. seive No. 9, more than

a. 10%

b. 15%

c. 20%

d. 25%

Explanation: Option A is correct.

130. The top diameter, bottom diameter and the height of a slump mould are :

a. 10 cm, 20 cm, 30 cm

b. 10 cm, 30 cm, 20 cm

c. 20 cm, 10 cm, 30 cm

d. 20 cm, 30 cm, 10 cm

Explanation: Option A is correct.

131. Workability of concrete mix with low water cement ratio is determined by

a. slump test

b. compaction factor test

c. flexural strength test

d. none of these.

Explanation: Option B is correct.

Series of low to high.
1. Vee bee.
2. Compaction factor.
3. Slump.
4. Flow test.
According To option, compaction is correct.

132. While designing an air entrained concrete

a. proportion of aggregates is reduced

b. an allowance for the entrained air is made

c. strength of the concrete, is reduced

d. all the above.

Explanation: Option D is correct.

133. Pick up the incorrect statemnt from the following. For performing compressive strength test of cement

a. cement and standard sand mortar are used in the ratio of 1 : 3

b. water is added at the rate of  + 3.0 percentage of water where P is the percentage of water for standard consistency

c. A cube mould of 10 cm x 10 cm x 10 cm is used

d. The perpared moulds are kept in a atmosphere of 50% relative humidity

Explanation: Option A is correct.

D is in correct, but yes concrete is tested in 10*10*10 mould but compressive strength of 10*10*10 is more than stand design concrete.

134. For concreting tunnel linings, tran-portation of concrete is done by

a. wheel borrows

b. containers

c. pumps

d. belt conveyors.

Explanation: Option C is correct.

135. The operation of removing humps and hollows of uniform concrete surface, is known as

a. screeding

b. trowelling

c. finishing

d. none of these.

Explanation: Option A is correct.

Floating is the removal of excess cement concrete. And screeding is done to fill hollow space and and make uniform appearance and then trowelling is done to finalise the surface to give smooth surface.

136. The void ratio of

a. single size coarse aggregate is roughly 0.45.

b. graded coarse aggregate is roughly 0.040

c. fine aggregate is roughly 0.45

d. all the above.

Explanation: Option D is correct.

137. The type of aggregates not suitable for high strength concrete and for pavements subjected to tension, is

a. rounded aggregate

b. irregular aggregate

c. angular aggregate

d. flaky aggregate

Explanation: Option A is correct.

138. For the construction of R.C.C. slabs, columns, beams, walls, etc. the grade of concrete mix used, is

a. 1 :  : 3

b. 1 : 2 : 4

c. 1 : 1 : 2

d. 1 : 4 : 8.

Explanation: Option B is correct.

1:1.5:3 is M20 grade of concrete. 1:2:4 is M20 Grade of Concrete & for RCC minimum M20 grade is use as per IS 456-2000.

139. The type of aggregates of same nominal size, which contain less voids when compacted, are

a. rounded spherical

b. irregular

c. flaky

d. none of these.

Explanation: Option A is correct.

The round aggregate has 30-35% void ratio which is minimum as compare to irregular and flaky so when we compact found lesser voids.

140. For the construction of cement con-certe dams, the maximum permissible size of the aggregates, is

a. 40 mm

b. 50 mm

c. 60 mm

d. 70 mm

Explanation: Option A is correct.

Cyclopean concrete is Used as massed concrete in place of pouring the concrete.
Massed concrete is also known as Or pudding.

141. Permissible compressive strength of M 200 concrete grade is

a. 150 kg/cm2

b. 200 kg/cm2

c. 250 kg/cm2

d. 300 kg/cm2

Explanation: Option B is correct.

142. For preparing a test-specimen, it is necessary

a. to mix coarse aggregates

b. to mix water to the cement, fine aggregates and coarse aggregates

c. to oil inner surface of the mould and the base plate, before placing concrete

d. all the above.

Explanation: Option D is correct.

143. The aggregate containing moisture in pores and having its suface dry, is known as

a. very dry aggregates

b. dry aggregates

c. saturated surface dry aggregate

d. none of these.

Explanation: Option C is correct.

144. The commercial name of white and coloured cement in India, is

a. rainbow cement

b. silvicrete

c. snowcem

d. all the above.

Explanation: Option D is correct.

145. Pick up the correct statement from the following:

a. Angular and rough aggregates reduce the workability of the concrete

b. Large size aggregates increase the workability due to lesser surface area

c. The slump of the concrete mix decreases due to an increase in temperature

d. All the above.

Explanation: Option D is correct.

146. To hydrate 500kg of cement full water needed, is

a. 110 kg

b. 120 kg

c. 130 kg

d. 140 kg

Explanation: Option C is correct.

It has been further estimated that about 15% by weight of cement is required to fill up the gel pores and 23% is used for hydation of cement process. So total 38% is required.

147. Concrete gains strength due to

a. chemical reaction of cement with sand and coarse aggregates

b. evaporation of water from concrete

c. hydration of cement

d. All the above.

Explanation: Option C is correct.

The reaction b\w cement and water is called hydration and heat produce during hydration is called heat of hydration thats why concrete gains strength due to hydration of cement.

148. If aggregates completely pass through a sieve of size 75 mm and are retained on a sieve of size 60 mm, the particular aggregate will be flaky if its minimum dimension is less than

a. 30.5 mm

b. 40.5 mm

c. 50.5 mm

d. none of these.

Explanation: Option B is correct.

Flaky aggregate = 3/5 of there's mean dimension.
                            = (3/5) *{(75+60) /2}.
                           = (3/5) *(67.5).
                            = 40.5mm.

149. Non-uniform compaction may cause the concrete

a. porous

b. non-homogeneous

c. reduced strength

d. all the above.

Explanation: Option D is correct.

150. Log Angles machine is used to test the aggregate for

a. impact value

b. abrasion resistance

c. water absorption

d. none of these.

Explanation: Option B is correct.

151. If fineness modulus of sand is 2.5, it is graded as

a. fine sand

b. medium sand

c. coarse sand

d. very coarse sand.

Explanation: Option A is correct.

Fine aggregates range from a FM of 2.00 to 4.00, and coarse aggregates smaller than 38.1 mm range from 6.50 to 8.00. Combinations of fine and coarse aggregates have intermediate values.

152. Pozzolanic properties exist in

a. fly ash

b. pumicite

c. diatomaceous clay

d. all the above.

Explanation: Option D is correct.

153. An aggregate which passes through 25 mm I.S. sieve and is retained on 20 mm sieve, is said to be flaky if its least dimension is less than

a. 18.5 mm

b. 16.5 mm

c. 15.5 mm

d. 13.5 mm.

Explanation: Option D is correct.

20+25 = 45.
45/2 = 22.5.
As know agg are flaky when least dimension is 3/5.
So, 22.5*3/5 = 13.5.

154. Expansion joints are provided if the length of concrete structures exceeds

a. 15 m

b. 15 m

c. 35 m

d. 45 m

Explanation: Option D is correct.

Expansion and contraction joints are provided if the length of concrete structures exceeds 12 meters in length.
Reference: R Agore.

155. Workability improved by adding

a. hydrated lime

b. calcium chloride

c. bentonite

d. all the above.

Explanation: Option D is correct.

156. If the slump of a concrete mix is 60 mm, its workability is

a. low

b. medium

c. high

d. none of these.

Explanation: Option B is correct.

The degree of workability of concrete and its slump values are;
(1) Very Low 0 - 25 mm slump
(2) Low 25-50 mm slump.
(3) Medium 50-100 mm slump.
(4) High 100-150 mm slump.

157. Pick up the correct statement from the following:

a. Sand obtained from flooded pits, need not be washed before use

b. Sea shore sand contains chlorides which cause effloresance

c. The chloride in sea shore sand and shingle may cause corrosion of reinforcement if the concrete is porous

d. All the above.

Explanation: Option D is correct.

158. The strength and quality of concrete, depend upon:

a. surface area of aggregates

b. shape of aggregates

c. surface texture of aggregates

d. all the above.

Explanation: Option D is correct.

All the parameters mentioned above affect the strength and quality of the concrete, viz. Grading, surface area, texture and shape of aggregates.

159. The process of mixing, transporting, placing and compacting concrete using Ordinary Port land Cement should not take more than

a. 30 minutes

b. 40 minutes

c. 60 minutes

d. 75 minutes

Explanation: Option A is correct.

160. Pick up the incorrect statement from the following. While performing preliminary test on concrete

a. cement should be mixed by hand in order to maintain uniformity

b. concrete mix should be stored in air-tight containers

c. concrete ingredients should be kept at a temperature of 37° ± 2°C

d. none of these.

Explanation: Option C is correct.

161. Sand requiring a high water cement ratio, belongs to

a. Zone I

b. Zone II

c. Zone III

d. Zone IV.

Explanation: Option A is correct.

Aswer should be zone 4. Zoning start from coarser to finer. So, zone 4 is the finer one. For finer sand surface area is more so more high water cement ratio.

162. Ordinary Portland cement is manufactured from

a. lime stone and clay

b. gypsum and lime

c. pozzolana

d. lime, pozzolana and clay.

Explanation: Option B is correct.

A is correct lime stone (calcareous) and clay (aluminum, silica, ferric oxides) because 5% of gypsum is added just to overcome quick setting of cement.

163. A flaky aggregate is said to be elongated if its length is

a. twice the mean size

b. thrice the mean size

c. four times the mean size

d. five times the mean size.

Explanation: Option A is correct.

Mean of flaky aggregate is (3+5) /2=4.
Ellongated agg. 5/8.
So elongated length 8 but mean of flaky 4.
Then 2 times.

164. To prevent segregation, the maximum height for placing concrete, is

a. 100 cm

b. 125 cm

c. 150 cm

d. 200 cm

Explanation: Option A is correct.

As per clause 13.2 of IS 456: 2000, the maximum permissible free fall of concrete to avoid segregation may be taken as 1.5 m or 150 cm.

165. If the various concrete ingredients i.e. cement, sand and aggregates are in the ratio of 1:3:6, the grade of concrete, is

a. M 100

b. M 150

c. M 200

d. M 250

Explanation: Option A is correct.

166. Water cement ratio is generally expressed in volume of water required per

a. 20 kg

b. 30 kg

c. 40 kg

d. 50 kg

Explanation: Option D is correct.

167. For a good concrete

a. cement should be sufficient to produce the required strength

b. water should be free from organic materials

c. mixing of ingredients should be done thoroughly so as to produce homogeneity

d. All the above.

Explanation: Option D is correct.

168. If the effective plan area of a warehouse is 54 sq. m, and maximum height of piles permitted is 270 cm, the number of cement bags to be stored, is

a. 2200 bags

b. 2400 bags

c. 2700 bags

d. 3000 bags

Explanation: Option C is correct.

Simply,
No. Of bags = Effective area* Max.ht of piles/ Area coverd by one bag cement is 0.3 sq.m & ht= 0.18.
No= 54*2.7/0.3*0.18 = 2700 bags you must get.

169. Gypsum is added for

a. colour

b. strength

c. controlling setting time

d. none of these.

Explanation: Option C is correct.

170. A concrete having a slump of 6.5 cm, is said to be

a. earth moist

b. semi-plastic

c. plastic

d. none of these.

Explanation: Option C is correct.

In RCC code only three stages are given:-.
Slump 0 (Solid mix) , 0-40mm (Semi plastic mix) and 40-150mm (Plastic mix).

171. Strength of concrete with passage of time

a. increases

b. decreases

c. fluctuates

d. remains constant.

Explanation: Option A is correct.

Simply, the strength of concrete with the passage of time increase and strength of cement with the passage of time decrease.

172. Cement used for normal concrete construction, is obtained by burning a mixture of

a. argilaceous and calcareous materials

b. silicious and catcareous materials

c. silicious, argillaceous and calcareous materials

d. none of these.

Explanation: Option C is correct.

It is given on the base of coefficient of expansion.
Silicious = high coefficient of expantion.
Argillaceous = medium.
Calcareous = less.

173. Pick up the correct statement from the following:

a. The concrete cured at a temperature below 23°C, gains strength up to 28 days

b. The concrete does not set at freezing point

c. The strength of concrete increases with its age

d. All the above.

Explanation: Option D is correct.

174. Pick up the incorrect statement from the following:

a. Admixtures accelerate hydration

b. Admixtures make concrete water proof

c. Admixtures make concrete acid proof

d. Admixtures give high strength

Explanation: Option A is correct.

Admixture may affect the acceleration or retardation effects in scence of setting time (having any form or shape) rather than hydration (gaining strength).

175. Higher workability of concrete is required if the structure is

a. made with cement concrete

b. thick and reinfored

c. thin and heavily reinforced

d. thick and heavily reinfored.

Explanation: Option D is correct.

Option C is correct because it is not properly possible to do compaction of harsh concrete in thin and heavily reinforced section.

176. Setting time of cement increases by adding

a. gypsum

b. hydrogen peroxide

c. calcium chloride

d. sodium oxide

Explanation: Option A is correct.

Gypsum is a retarder:it means setting time increase and reduce early setting of cement.
Accelerator: as the name indicate it increase the setting and decrease setting time.

177. The dimensions of a 35 litre forma for measuring aggregates by volume, are :

a. length 39 cm, breadth 25 cm, height 32 cm

b. length 27 cm, breadth 27 cm, height 48 cm

c. length 220 cm, breadth 25 cm, height 40 cm

d. none of these.

Explanation: Option B is correct.

178. The shuttering of a hall measuring 4 m x 5 m, can be removed after

a. 7 days

b. 10 days

c. 14 days

d. 21 days

Explanation: Option A is correct.

According to IS code 456.
Props to the slab.
1) Spanning up to 4.5m --> 7days.
2) Spanning over 4.5m  --> 14 days.
So for the longer span of 4m * 5m slab --> 14 days.

179. Pick up the correct statement from the following:

a. Cement should be mixed for at least one minute

b. 10% of water is placed in the rotating drum before adding dry material

c. 10% of water is added after placing the other ingredients in the drum

d. All the above.

Explanation: Option D is correct.

180. If 50 kg of fine aggregates and 100 kg of coarse agregates are mixed in a concrete whose water cement ratio is 0.6, the weight of water required for harsh mix, is

a. 10 kg

b. 12 kg

c. 14 kg

d. 15 kg.

Explanation: Option B is correct.

Here 50 kg weight of cement:
M 25 ratio 1:1:2.
(5% weight of aggregate + 30 weight of cement)w/c ratio.

181. The entrained air in concrete

a. increases workability

b. decreases workability

c. decreases resistance to weathering

d. increases strength

Explanation: Option A is correct.

Air-entrained concrete contains billions of microscopic air cells per cubic foot. These air pockets relieve internal pressure on the concrete by providing tiny chambers for water to expand into when it freezes.

182. Pick up the incorrect statement from the following:

a. Tricalcium silicate (C3S) generates more heat of hydration

b. Tricalcium silicate (C3S) develops early strength

c. Tricalcium silicate (C3S) has more resistance to sulphate attack

d. None of these.

Explanation: Option C is correct.

183. Permissible compressive strength of M 200 concrete grade is

a. 150 kg/cm2

b. 200 kg/cm2

c. 250 kg/cm2

d. 300 kg/cm2

Explanation: Option B is correct.

Characteristic compressive strength of M200 grade cement is 200 kg/cm^2.
Permissible compressive strength of M200 grade concrete is (200 ÷ 1.5) = 133.3 kg/cm^2.
Design strength of M200 grade concrete is (133.3 ÷ 1.5) = 88.8 kg/cm^2.

184. In slump test, each layer of concrete is compacted by a steel rod 60 cm long and of 16 mm diameter for

a. 25 times

b. 30 times

c. 40 times

d. 50 times

Explanation: Option A is correct.

It belongs to the slump cone test. Use to find the workability of concrete. In which concrete fill in the slump cone in 3 layers and compact with the steel rod 25 times of each layer.

185. If the average compressive strength is 4000 kg/cm2 and standard deviation is 500, the co-efficient of variation is

a. 12.5%

b. 15%

c. 18.5 %

d. 20%

Explanation: Option A is correct.

Co-efficient of variation = (Standard deviation/Avg.strength of concrete) * 100.
= 500/4000 * 100,
= 12.5.

186. For preparing ordinary concrete, the quantity of water used, is

a. 10% by weight of aggregates plus 10% of weight of cement

b. 5% by weight of aggregates plus 30% of weight of cement

c. 30% by weight of aggregates plus 10% of weight of cement

d. none of these.

Explanation: Option B is correct.

38% water by weight of cement is required for complete hydration of cement and to fill gel pores so the correct option is C.

187. According to IS : 382-1963, a good aggregate should be

a. chemically inert

b. sufficiently strong

c. hard and durable

d. all the above.

Explanation: Option D is correct.

188. The 28 days cube strength of mass concrete using aggregates of maximum size 5 cm for gravity dams should be

a. between 350 to 600 kg/cm2

b. between 150 to 500 kg/cm2

c. below 200 kg/cm2

d. none of these.

Explanation: Option C is correct.

In mass concrete low setting like foundation concrete which is below M20 concrete so strength can be below or not more than 200.

189. If P, Y and Z are the weights of cement, fine aggregates and coarse aggregates respetively and W/C is the water cement ratio, the minimum quantity of water to be added to first batch, is obtained by the equation

a. 0.3P + 0.1Y + 0.01Z = W/C x P

b. 0.4P + 0.2Y + 0.01Z = W/C x P

c. 0.5P + 0.3Y + 0.01Z = W/C x P

d. 0.2P + 0.5Y + 0.1Z = W/C x P

Explanation: Option A is correct.

190. For the construction of thin R.C.C. structures, the type of cement to be avoided, is

a. rapid hardening cement

b. low heat cement

c. blast furnace slag cement

d. sulphate resisting cement.

Explanation: Option C is correct.

It should be low heat cement because low heat cement has coarser particles which are not properly spread in thin RCC structure.

191. Vicat apparatus is used for

a. consistency test

b. test for setting time

c. test for tensile strength

d. none of these.

Explanation: Option A is correct.

192. Pick up the incorrect statement from the following:

a. Cement bags should preferably be piled on wooden planks

b. Cement bags should be placed such that bags of one layer does not touch the bags of the adjacent layer

c. Width and height of the pile should not exceed 3 m and 2.70 m respectively

d. None of these.

Explanation: Option D is correct.

A and C both options incorrect.
A space of 600 mm minimum shall be left between the exterior walls and the stack.

193. For the construction of the retaining structures, the type of concrete mix to be used, is

a. 1 : 2 :4

b. 1 :  : 3

c. 1 : l : 2

d. 1 : 4 : 8.

Explanation: Option B is correct.

194. An ideal ware house, is provided

a. water proof roof

b. few windows which remain generally closed

c. 15 cm thick concrete floor laid on a dry course of soling

d. all the above.

Explanation: Option D is correct.

195. Concrete is unsuitable for compaction by a vibrator if it is

a. earth moist

b. semi-plastic

c. plastic

d. none of these.

Explanation: Option C is correct.

If concrete is plastic, then its workability will be high. In such causes vibrator is not a suitable technique for compaction.

196. Inert material of a cement concrete mix, is

a. water

b. cement

c. aggregate

d. none of these.

Explanation: Option C is correct.

The word Inert means not reacting with any other things even with favorable conditions. So the aggregate doesn't react chemically with cement and water if there is nothing chemical present in it.

197. Sands of zone I are

a. coarse

b. medium

c. medium to fine

d. fine.

Explanation: Option A is correct.

Zone I - Coarse Sand.
Zone II - Normal Sand.
Zone III - Fine Sand.
Zone IV - Very Fine Sand.

198. The lower water cement ratio in concrete, introduces

a. greater density and smaller permeability

b. improved frost resistance

c. greater wear resistance and improved bond strength

d. all the above.

Explanation: Option D is correct.

199. The cement becomes useless if its absorbed moisture content exceeds

a. 2%

b. 3%

c. 4%

d. 5%

Explanation: Option D is correct.

200. A concrete using an air entrained cement

a. has more resistance to weathering

b. is more plastic and workable

c. is free from segregation and bleeding

d. all the above.

Explanation: Option B is correct.

Segregation and bleeding does not depend on the type of cement so option E is not correct. Furthermore it should also be clear that if concrete has voids than it has no good resistance to weathering agents.

201. Pick up the correct statement from the following:

a. The maximum size of the fine aggregate, is 4.75 mm and minimum 0.075 mm

b. The material having particles of size varying from 0.06 mm to 0.002 mm, is known as silt

c. The material having particles of size less than 0.002 mm, is known as clay

d. All the above.

Explanation: Option D is correct.

202. Placing of concrete should preferably be done at a temperature of

a. 10°C

b. 20°C

c. 23°C

d. 27 ± 2°C

Explanation: Option D is correct.

203. The aggregate impact value of the aggregate used in

a. building concrete is less than 45

b. road pavement concrete is less than 30

c. runway concrete is less than 30

d. all the above.

Explanation: Option D is correct.

The aggregate impact value is a measure of resistance to sudden impact or shock, which may differ from its resistance to gradually applied compressive load.

204. The maximum percentage of chemical ingredient of cement is that of

a. iron oxide

b. aluminium

c. lime

d. silica.

Explanation: Option C is correct.

Lime (CaO)	60 to 67%
Silica (SiO2)	17 to 25%
Alumina (Al2O3)	3 to 8%
Iron oxide (Fe2O3)	0.5 to 6%
Magnesia (MgO)	0.1 to 4%
Sulphur trioxide (SO3)	1 to 3%
Soda and/or Potash (Na2O+K2O)	0.5 to 1.3%

205. Pick up the incorrect statement from the following:

a. Concrete for which preliminary tests are conducted, is called controlled concrete

b. Bulking of sand depends upon the fineness of grains

c. Concrete mix 1 : 6 : 12, is used for mass concrete in piers.

d. All the above.

Explanation: Option D is correct.

206. Sand generally contains salt if it is obtained from:

a. river beds

b. sea beds

c. all the above

d. none of these.

Explanation: Option B is correct.

207. The impurity of mixing water which affects the setting time and strength of concrete, is

a. sodium chlorides

b. sodium carbonates and bicarbonates

c. calcium chorides

d. calcium bicarbonates

Explanation: Option B is correct.

Sodium carbonate and bi carbonate causes temporary hardness for this reason effect of harness and setting time of concrete.

208. Pick up the correct statement from the following:

a. Continuous grading is not necessary for obtaining a minimum of air voids

b. The omission of a certain size of aggregate is shown by a straight horizontal line on the grading curve

c. The omission of a certain size of aggregate in concrete increases the workability but also increases the liability to segregation

d. All the above.

Explanation: Option D is correct.

209. Di-calcium silicate (C2S)

a. generates less heat of hydration

b. hardens rapidly

c. provides less ultimate strength to cement

d. has less resistance to sulphate attack.

Explanation: Option A is correct.

210. On a grading curve, the gap grading is represented by

a. a horizontal line

b. a vertical line

c. N.W. inclined line

d. N.E. inclined line

Explanation: Option A is correct.

Gap grading means certain fraction of sizes are not present in the aggregate sizes and hence because of that a horizontal line is used to represent the absent fractions (sizes) in a grading curve.

211. Bulking of sand is

a. mixing of different sizes of sand particles

b. mixing of lime with sand

c. maximum water with sand

d. swelling of sand when wetted.

Explanation: Option D is correct.

212. Curing of pavements, floors, roofs and slabs, is done by

a. ponding method

b. covering surface with bags

c. sprinkling water method

d. shading concrete method.

Explanation: Option A is correct.

Ponding method is generally adopted for curing of floors, roofs, slabs. Sprinkling of water is adopted for column and membrane method is adopted at scarcity of water. Covering surface with bags is done for columns and cubes testing.

213. Pick up the incorrect statement from the following:

a. With passage of time, the strength of cement increases

b. With passage of time, the strength of cement decreases

c. After a period of 24 months, the strength of cement reduces to 50%

d. The concrete made with storage deteriorated cement, gains strength with time

Explanation: Option A is correct.

According to me, the expiridate of cement is 3 months. After a period, 24 month reduces 50 percentage is wrong.

214. The surface where two successive placements of concrete meet, is known as

a. Expansion joint

b. Construction joint

c. both (a) and (b)

d. both (6) and (c).

Explanation: Option B is correct.

215. An excess of flaky particles in concrete aggregates

a. increases the quantity of water and sand

b. affects the durability of concrete

c. more than 15% are not desirable

d. all the above.

Explanation: Option D is correct.

Flaky Aggregate :- The aggregate is said to be flaky when its least dimension is less than 3/5th (or 60%) of its mean dimension. Mean dimension is the average size through which the particles pass and the sieve size on which these are retained.

216. 1.S.I. has specified the full strength of concrete after

a. 14 days

b. 21 days

c. 28 days

d. 35 days

Explanation: Option C is correct.

217. For given workability the grading requiring the least amount of water is one that gives

a. greatest surface area for the given cement and aggregates

b. least surface area for the given cement and aggregates

c. least weight for the given cement and aggregates

d. greatest weight for the given cement and aggregates

Explanation: Option A is correct.

218. The minimum percentage of chemical ingredient of cement is that of

a. magnesium oxide

b. iron oxide

c. alumina

d. lime

Explanation: Option A is correct.

Lime (CaO) ---> 60 to 67%.
Silica (SiO2) ---> 17 to 25%.
Alumina (Al2O3) ---> 3 to 8%.
Iron oxide (Fe2O3) ---> 0.5 to 6%.
Magnesia (MgO)	 ---> 0.1 to 4%.

219. The specifications of a cement bag for storage, are

a. height 18 cm

b. plan area 3000 sq. cm

c. volume 35 litres

d. all the above.

Explanation: Option D is correct.

220. The bulk density of aggregates, depends upon

a. shape

b. grading

c. compaction

d. all the above.

Explanation: Option D is correct.

221. Pick up the correct statement from the following:

a. The specific gravity of aggregate is important for the determination of the moisture content

b. The absorption and porosity of an aggregate influence the property of the concrete

c. A highly absorptive aggregate reduces the workability of concrete considerably

d. All the above.

Explanation: Option D is correct.

222. Horizontal construction joints in concrete walls are generally provided at

a. soffit level

b. window sill level

c. floor level

d. all the above.

Explanation: Option D is correct.

223. Pick up the correct statement from the following:

a. Construction joints in columns are provided at the bottom haunching

b. Construction joints in beams and slabs are provided within middel third

c. Constructionjoints are generally provided in positions subjected to least shear force

d. All the above.

Explanation: Option D is correct.

224. For a concrete mix 1:3:6 and water cement ratio 0.6 both by weight, the quantity of water required per bag, is

a. 12 kg

b. 14 kg

c. 16 kg

d. 20 kg

Explanation: Option B is correct.

Water required = (5% of aggregate + 30% of cement) * w/c.
Cement per bag = 50 kg.
Aggregate = 50*3 = 150 kg.
5% of aggregate = 7.5 kg.
30% of cement= 15 kg.
Water required = (15+7.5)*0.6 = 13.5 kg which may be approximately 14 kg.

225. The concrete mix which causes difficulty in obtaining a smooth finish, possess

a. internal friction

b. harshness

c. bleeding

d. none of these.

Explanation: Option B is correct.

226. Le-Chatelier's apparatus is used for testing

a. soundness of cement

b. hardness of cement

c. strength of cement

d. durability of cement.

Explanation: Option A is correct.

227. 'Ware house pack' of cement means

a. pressure exertion of the bags of upper layers

b. pressure compaction of the bags on lower layers

c. packing the ware house

d. none of these.

Explanation: Option B is correct.

As in ware house the cement bags are piled upto max height of 3m so the lower bags are get compacted by overlain bags hence option is correct.

228. In the method of voids for determination of the quantity of cement paste, it is assumed that

a. Voids in fine aggregates are filled by the cement paste

b. Volume of fine aggregates is equal to total voids in coarse aggregates plus 10% extra

c. Volume of cement paste required is equal to total volume of voids in fine aggregates plus 15% extra

d. All the above.

Explanation: Option D is correct.

229. If a grading curve is horizontal bet-wen the portions of 20 mm I.S. Sieve and 4.75 mm I.S. Sieve, the graded aggregates do not contain

a. 20 mm particles

b. 10 mm particles

c. 4.75 mm particles

d. all the above.

Explanation: Option D is correct.

Horizontal curves grading mean where is it starting and ending it mean those particles between them is missing.
Ex starting 4.75mm ending 20 mm.
i.e 4.75 to 20mm particles are Missing in aggregate.

230. The size of fine aggregates does not exceed

a. 3.00 mm

b. 3.75 mm

c. 4.75 mm

d. 5.75 mm

Explanation: Option C is correct.

231. An aggregate is known as cyclopean aggregate if its size is more than

a. 30 mm

b. 60 mm

c. 75 mm

d. 90 mm.

Explanation: Option C is correct.

232. The main object of compaction of concrete, is:

a. to eliminate air holes

b. to achieve maximum density

c. to provide initimate contact between the concrete and embedded materials

d. all the above.

Explanation: Option D is correct.

233. Pick up the correct statement from the following:

a. The quantity of water required for concreting, depends upon the grading of aggregate amd method of compaction

b. 10% excess of water reduces the strength of concrete by 15%

c. 30% excess of water reduces the strength of concrete by 50%

d. All the above.

Explanation: Option D is correct.

234. Particles of 0.002 mm size are that of

a. clay

b. sand

c. gravel

d. none of these.

Explanation: Option A is correct.

CLAY  :   <0.002mm.
SILT    :    0.002-0.06mm.
SAND  :   0.06-2mm.
GRAVEL :   2-20mm.
BOULDER :   >20mm.
FINE AGGREGATE SIZE :  <4.75mm.
COURSE AGGREGATE SIZE :  4.75 -75mm.
CYCLOPEAN AGGREGATE : >75mm.